# Oelex OX-210 High Impact Acoustical Wall Panel Specification for

# 1 1/8” & 2 1/8” Thick Panels

SECTION 09840 – ACOUSTICAL WALL PANELS

PART 1 – GENERAL

1.1	SUMMARY

- This section includes the following:

- Acoustical Wall Panel

  - SUBMITTALS

- Shop Drawings: Show fabrication and installation details for acoustical wall panels, including plans, elevations, sections, details and attachment to other work.

- Submittals:  Furnish 12” x 12” samples, showing manufacturer full range of colors, texture and patterns available for each type of acoustical product specified.

- Product Test Report: From a qualified testing agency indicating wall panels comply with requirements.

- Qualification Data: For firms specified in “Quality Assurance” Article to demonstrate their capabilities and experience.

- Product Certificates: Signed by manufacturer certifying that the products furnished comply with requirements.

  - QUALITY ASSURANCE

- Manufacturer Qualification: Manufacturer shall have a minimum of 5 years experience in production of specified products and shall furnish supporting documentation showing completed jobs of approximately the same size and scope.

- Fire Test Reports: Provide acoustical wall panels with the following surface- burning characteristics as per ASTM E 84.

- Flame Spread: 25 or less

- Smoke Developed: 450 or less

- Acoustical Test Report: Provide acoustical test report from a qualified testing agency indicating acoustical wall panels meets 0.65 – 1.05 NRC per ASTM C-423.

  - DELIVERY, STORAGE, AND HANDLING

- Protect Acoustical Wall Panels from excessive moisture when shipping, storing, and handling.  Deliver in unopened skids and store in a dry place with adequate air circulation.  Do not deliver material until all wet-work has been completed.

PART 2 – PRODUCTS

  - WALL PANELS, GENERAL

- Acoustical Wall Panels shall be 1 1/8”, or 2 1/8”thick 6.0-7.0 lb. per cubic foot high-density fine fibered fiberglass bonded to a 1/8” thick high impact 16-20 lb. per cubic foot high density impact / tackable molded fiberglass board.   Manufacturer’s standard panel construction fully wrapped and hardened edges, with panel manufacturer’s standard full line of fabric.

- Products

- Model # Oelex OX-210

Oeler Industries, Inc.

Pittsburgh, PA.  USA

Ph. (412) 884-3000

Fax (412) 884-3300

- Facing Material: Guilford of Maine FR 701 – Style 2100 – 100% polyester (or other)

- Panel Thickness: nominal (1 1/8”, 2 1/8”) thick

- Noise Reduction Coefficient:  NRC 0.85 – 1.15

- Panel Width: 48 inches

- Panel Length: As indicated, up to 10 feet long.

  - CONSTRUCTION

- The acoustical wall panel product shall be supplied in 48” wide panels with lengths as indicated.  All edges will be fully wrapped with mounting as indicated.

  - MOUNTING

A.	Back-Mounting Accessories: Manufacturers standard accessories for securely mounting panels, of type and size indicated and complying with the following requirements:

- Mechanically Mounted Edge-Reinforced Panels: Metal clips designed to support weight of panels, mechanically attached to wall substrate according to manufacturers standard pattern and adhesively bonded to back of panel, with base support brackets where recommended by manufacturer for additional support of panels.

- Two Part Mechanical Clip: One part mechanically attached to wall substrate, one part impaled into and bonded to the back of panel, with leveling base to support brackets where indicated.

2.4	ACOUSTICAL PERFORMANCE – 1 1/8” Panels

Sound Absorption: Per ASTM C – 423

Sound Absorption Coefficient per Octave Band Center Frequency (Hz)

125	250	500	1000	2000	4000		NRC

0.14	0.27	0.80	1.11	1.14	1.14		0.85

ACOUSTICAL PERFORMANCE – 2 1/8” Panels

Sound Absorption: Per ASTM C – 423

Sound Absorption Coefficient per Octave Band Center Frequency (Hz)

125	250	500	1000	2000	4000		NRC

0.22	0.81	0.80	1.24	1.30	1.16		1.15

2.5	FLAMMABILITY RATING

- All components shall have a Class A Flammability rating per ASTM E- 84:  Surface Burning Characteristics of Building Materials, with a Flame Spread of 25 or less and Smoke Developed of 450 or less

PART 3 – EXECUTION

  - INSTALLATION

- Install Acoustical Wall panels in locations indicated, top edges level and in alignment with other panels.   Comply with manufacturers written instructions for installation of panels using type of mounting accessories indicated or, if not indicated, as recommended by manufacturer.

  - CLEANING

- After completion of installation of panels, remove dust and other foreign material according to manufacturers written instructions.

- Remove surplus material, rubbish, and debris resulting from panel installation, on completion of the work, and leave areas of installation in a neat and clean condition.