Specification for 1” thick OELEX O-CLD Ceiling Cloud Absorber

SECTION 09840 – ACOUSTICAL CEILING CLOUDS

PART 1 – GENERAL

1.1	SUMMARY

- This section includes the following:

- Ceiling Cloud

  - SUBMITTALS

- Shop Drawings: Show fabrication and installation details for Ceiling Cloud, including plans, elevations, sections, details and attachment to other work.

- Submittals:  Furnish 12” x 12” samples, showing manufacture full range of colors, texture and patterns available for each type of acoustical product specified.

- Product Test Report: From a qualified testing agency indicating Ceiling Clouds comply with requirements.

- Qualification Data: For firms specified in “Quality Assurance” Article to demonstrate their capabilities and experience.

- Product Certificates: Signed by manufacturer certifying that the products furnished comply with requirements.

  - QUALITY ASSURANCE

- Manufacturer Qualification: Manufacture shall have a minimum of 5 years experience in production of specified products and shall furnish supporting documentation showing completed jobs of approximately the same size and scope.

- Fire Test Reports: Provide Ceiling Clouds with the following surface- burning characteristics as per ASTM E 84.

- Flame Spread: 25 or less

- Smoke Developed: 450 or less

- Acoustical Test Report: Provide acoustical test report from a qualified testing agency indicating acoustical wall panels meets 0.85 NRC per ASTM C-423.

  - DELIVERY, STORAGE, AND HANDLING

- Protect Ceiling Clouds from excessive moisture when shipping, storing, and handling.  Deliver in unopened skids and store in a dry place with adequate air circulation.  Do not delivery material until all wet-work has been completed.

PART 2 – PRODUCTS

  - CEILING CLOUDS, GENERAL

- Ceiling Clouds shall be 1” thick – 6.0-7.0 lb. per cubic foot high-density fine fibered fiberglass.   Manufactures standard panel construction, fully wrapped hardened, panel manufactures standard full line of fabric.

- Products

- Model # OELEX C-CLD200 Ceiling Cloud

Oeler Industries, Inc.

Pittsburgh, PA 15236

Ph. (877) 406-6473

Fax (412) 884-3000

- Facing Material: Guilford of Maine FR 701 – Style 2100 – 100% polyester

- Panel Thickness: nominal 1” thick

- Noise Reduction Coefficient:  NRC 0.85

- Panel Width: 48 inches

- Panel Length: As indicated, up to 10 feet long.

  - CONSTRUCTION

- The O-CLD200 Ceiling Cloud shall be supplied in 48” wide panels with lengths as indicated.  All edges will be fully wrapped with mounting as indicated.

  - MOUNTING

A.	Back-Mounting Accessories: Manufactures standard accessories for securely mounting ceiling clouds, of type and size indicated and complying with the following requirements:

- Mechanically Mounted T grid supports shall be secured into epoxy hardener spots. Minimum spacing of 24” between rows of T Grid.  Eyehooks secured into epoxy spots will not be accepted for Clouds over 48” x 48” size.

2.4	ACOUSTICAL PERFORMANCE

Sound Absorption: Per ASTM C – 423

Sound Absorption Coefficient per Octave Band Center Frequency (Hz)

125	250	500	1000	2000	4000		NRC

0.14	0.27	0.80	1.11	1.14	1.14		0.85

2.5	FLAMMIBILITY RATING

- All components shall  have a Class A Flammability rating per ASTM E- 84:  Surface Burning Characteristics of Building Materials, with a Flame Spread of 25 or less and Smoke Developed of 450 or less

PART 3 – EXECUTION

  - INSTALLATION

- Install Ceiling Clouds panels in locations indicated, top edges level and in alignment with other Clouds.   Comply with manufactures written instructions for installation of panels using type of mounting accessories indicated or, if not indicated, as recommended by manufacture.

  - CLEANING

- After completion of installation of panels, remove dust and other foreign material according to manufactures written instructions.

- Remove surplus material, rubbish, and debris resulting from panel installation, on completion of the work, and leave areas of installation in a neat and clean condition.

Specification for 2” thick OELEX O-CLD Ceiling Cloud Absorber

SECTION 09840 – ACOUSTICAL CEILING CLOUDS

PART 1 – GENERAL

1.1	SUMMARY

- This section includes the following:

- Ceiling Cloud

  - SUBMITTALS

- Shop Drawings: Show fabrication and installation details for Ceiling Cloud, including plans, elevations, sections, details and attachment to other work.

- Submittals:  Furnish 12” x 12” samples, showing manufacture full range of colors, texture and patterns available for each type of acoustical product specified.

- Product Test Report: From a qualified testing agency indicating Ceiling Clouds comply with requirements.

- Qualification Data: For firms specified in “Quality Assurance” Article to demonstrate their capabilities and experience.

- Product Certificates: Signed by manufacturer certifying that the products furnished comply with requirements.

  - QUALITY ASSURANCE

- Manufacturer Qualification: Manufacture shall have a minimum of 5 years experience in production of specified products and shall furnish supporting documentation showing completed jobs of approximately the same size and scope.

- Fire Test Reports: Provide Ceiling Clouds with the following surface- burning characteristics as per ASTM E 84.

- Flame Spread: 25 or less

- Smoke Developed: 450 or less

- Acoustical Test Report: Provide acoustical test report from a qualified testing agency indicating acoustical wall panels meets 1.15 NRC per ASTM C-423.

  - DELIVERY, STORAGE, AND HANDLING

- Protect Ceiling Clouds from excessive moisture when shipping, storing, and handling.  Deliver in unopened skids and store in a dry place with adequate air circulation.  Do not delivery material until all wet-work has been completed.

PART 2 – PRODUCTS

  - CEILING CLOUDS, GENERAL

- Ceiling Clouds shall be 2” thick – 6.0-7.0 lb. per cubic foot high-density fine fibered fiberglass.   Manufactures standard panel construction, fully wrapped hardened, panel manufactures standard full line of fabric.

- Products

- Model # OELEX C-CLD200 Ceiling Cloud

Oeler Industries, Inc.

Pittsburgh, PA 15236

Ph. (877) 406-6473

Fax (412) 884-3000

- Facing Material: Guilford of Maine FR 701 – Style 2100 – 100% polyester

- Panel Thickness: nominal 2” thick

- Noise Reduction Coefficient:  NRC 1.15

- Panel Width: 48 inches or as indicated on drawings

- Panel Length: As indicated, up to 10 feet long.

- Edge Detail: Beveled

  - CONSTRUCTION

- The S-2000 Ceiling Cloud shall be supplied in 48” wide panels with lengths as indicated.  All edges will be fully wrapped with mounting as indicated.

  - MOUNTING

A.	Back-Mounting Accessories: Manufactures standard accessories for securely mounting ceiling clouds, of type and size indicated and complying with the following requirements:

- Mechanically Mounted T grid supports shall be secured into epoxy hardener spots. Minimum spacing of 24” between rows of T Grid.  Eyehooks secured into epoxy spots will not be accepted for Clouds over 48” x 48” size.

2.4	ACOUSTICAL PERFORMANCE

Sound Absorption: Per ASTM C – 423

Sound Absorption Coefficient per Octave Band Center Frequency (Hz)

125	250	500	1000	2000	4000		NRC

0.22	0.81	1.24	1.30	1.21	1.16		1.15

2.5	FLAMMIBILITY RATING

- All components shall  have a Class A Flammability rating per ASTM E- 84:  Surface Burning Characteristics of Building Materials, with a Flame Spread of 25 or less and Smoke Developed of 450 or less

PART 3 – EXECUTION

  - INSTALLATION

- Install Ceiling Clouds panels in locations indicated, top edges level and in alignment with other Clouds.   Comply with manufactures written instructions for installation of panels using type of mounting accessories indicated or, if not indicated, as recommended by manufacture.

  - CLEANING

- After completion of installation of panels, remove dust and other foreign material according to manufactures written instructions.

- Remove surplus material, rubbish, and debris resulting from panel installation, on completion of the work, and leave areas of installation in a neat and clean condition.