SPEC DATA SHEET # QFA-EXT-D2

4700 Clairton Blvd., Pittsburgh, PA 15236

Tel: (412) 884-3000

www.oeler.com

•

•

Fax: (412) 884-3300

sales@oeler.com

Intelligent Acoustic Solutions

QFA SERIES

QFA-EXT-D2

Oelex

Exterior

Grade

Quilted	Fiberglass

Absorbers by Oeler Industries, Inc. reduce the

reflection of sound waves by covering reflective surfaces with a suitable protected porous, open-celled material. QFA-EXT-D2 consists of a heavy-duty 10 oz per sq yd vinyl-coated-polyester (VCP) facing on both sides of a 2” thick quilted fiberglass.

Wall	panels	are	constructed	with	grommets

across the top and are

exterior grade thread.

sewn

with

Gore

Tenara

FEATURES:

•

•

Superior UV and weather resistance

Available facing colors on quilt: gray, tan, black, off-white

NRC rating 0.85

STC 21

•

•

Intelligent Acoustic Solutions

SPEC DATA SHEET # QFA-EXT-D2

APPLICATIONS:

Typically used to reduce reverberant noise on construction sites where the product may be subjected to sunlight, rain, snow, and winds. It is commonly installed over wood fencing or on brick or masonry walls of buildings adjacent to a job site or a noisy piece of machinery.

PRODUCT DATA DESCRIPTION:

Vinyl Coated Polyester (VCP) facing/ 2” fiberglass batt Vinyl Coated Polyester (VCP) facing

Nominal Thickness: 2.0 inches

Temperature Range: -400 to +1800 F

Standard Width: 48” wide Roll Length: 25’ long Weight: 0.50 lb psf

ACOUSTICAL PERFORMANCE:

Sound Absorption Performance:

OCTAVE BAND FREQUENCIES (HZ)

ASTM C 423

4700 Clairton Blvd., Pittsburgh, PA 15236

Tel: (412) 884-3000 • Fax: (412) 884.3300

www.oeler.com

•

sales@oeler.com

Intelligent Acoustic Solutions

Product	125	250	500	1K	2K	4K	NRC

QFA-EXT-D-2”	0.19	0.99	0.96	0.80	0.57	0.33	0.85