Intelligent Acoustic Solutions

# TONEWOOD 200

You only get one chance to make a first impression. With Oelex ToneWood 200 by Oeler Industries, Inc., it’s always a good one.

These acoustical panels are comprised of a wood veneered MDF board facing and a backing made from 100% Polyethylene Terephthalate (PET) a 100% recyclable material.

## COMPOSITION

Facing:

•Wood-veneered MDF board

- Backing:

- 100% Polyethylene Terephthalate (PET)

- 55% recycled content

## ENVIRONMENTAL FACTORS

- PET is 100% recyclable

- Low VOC emissions

- ASTM — D51116

- LEED — MRc4

# FEATURES:

## SPEC DATA SHEET # ToneWood-200

4700 Clairton Blvd., Pittsburgh, PA 15236

Tel: (412) 884-3000 • Fax: (412) 884-3300

www.oeler.com	•	sales@oeler.com

  - Quick & easy installation

  - Application on walls or ceilings

  - Cut to size in the field

  - Built-in spacers

  - Easy to handle

  - Linear design

  - Choice of 6 woodgrain veneers

4700 Clairton Blvd., Pittsburgh, PA 15236

Tel: (412) 884-3000 • Fax: (412) 884.3300

www.oeler.com	•	sales@oeler.com

Intelligent Acoustic Solutions

Intelligent Acoustic Solutions

## SPEC DATA SHEET #TONEWOOD-200

ACOUSTICAL DATA:

1/3 Octave Sound Absorption Coefficients at the Octave Band Frequencies

| Frequency (Hz) | 125 | 250 | 500 | 1000 | 2000 | 4000 | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 0.08 | 0.08 | 0.29 | 0.70 | 1.07 | 0.83 | 0.55 |
| Type “A” mount – flat |  |  |  |  |  |  |  |
| Frequency (Hz) | 125 | 250 | 500 | 1000 | 2000 | 4000 | NRC |
|  | 0.04 | 0.18 | 0.50 | 1.02 | 1.04 | 0.77 | 0.70 |
| Modified Type D-20 mount – 1” airspace |  |  |  |  |  |  |  |
| Frequency (Hz) | 125 | 250 | 500 | 1000 | 2000 | 4000 | NRC |
|  | 0.17 | 0.39 | 0.87 | 1.10 | 0.81 | 0.84 | 0.80 |

Modified Type D-50 mount – 2” airspace

## SPECIFICATIONS:

- Panel Size: 24” x 96”

- Thickness: 0.87”

- Weight: 35 lbs / panel

- Fire Rating: Class B per ASTM E-84-21a

## INSTALL METHODS:

- Wall: Furring strip, direct with screws & adhesive

- Ceiling: Furring strip